Azərbaycan Arxeologiyası 2000

Azerbaijan Archeology Vol.: 2 Num.: 3-4

THE STUDY OF RELATIONSHIP IN THE GLAZED EARTHENWARE TECHNOLOGICAL FEATURES IN THE CITIES OF NORTH AZERBAIJAN

Habib Teymuro\\ Hasanagha Ramazanli

(Azerbaijan AS the Institute of Archaeology and Ethnography)

Based on evident unity of cultures and on unification process, the cities of North Azerbaijan concentrated in themselves all kinds of highly developed and varied productions whose specialization and differentiation proceeded in separate handicrafts. Above mentioned factors favored the political, cultural and economic growth of such regional and multifunctional centers as Kabala, Barda, Shabran, Shamakha, Bandovan, Shamkhor, Gyandja, Balakan, Derbend, Sheki, Baylagan, Baku, etc. It must also be added that these centers occupied advantageous geographical situation, served as a binding link and a Trans - shipping point between the two major world and religious centers, were successors of cultural development of both regions.

Durability and longevity of ancient and medieval artistic and everyday ceramic wares is of certain scientific and practical interest. When excavating medieval towns they discovered in a great quantity fragments of monochromatic and polychromatic everyday glazed earthenwares. Methods of investigation of ceramic wares in 60-70-ies based on semi-facts and semi-conjectures do not correspond to up-to-date demands for reproduction of ancient production process. To determine relationship of technological features of fine faience production in mountainous and plain cities of North Azerbaijan, physico-chemical investigations such roeontgenospectral and spectral analyses have been carried out. Expediency of complex application of different analytic methods while investigating the analysis data is conditioned not only by the necessity of obtaining the most versatile information on local faience and its components ( kaolin, feldspar, oxides of different metals ) production but also by the task to investigate restoration of all technological conditions for its production in the Middle Ages.

Thorough investigation of technological conditions of fine glazed (0-1, 0-2 ), porous, fine grained, soft faience wares production affords us an opportunity to discover secrets of polyminerals and clay loams and solve the problem of faience production possibility in medieval North Azerbaijan. To ground this idea in up-to-date terms, it is necessary to study questions associated with materialogy, i.e. consider technological process in the Middle Ages. Composition of glazes found in everyday glazed earthenware is extremely divers and complex. By their chemical structure these glazes relate to compound silicates and aluminosilicates, oxides of different metals.On the basis of spectral and roentgenospectral analysis of faience glazes it has been established that glazed earthenware used in everyday life in medieval Shabran,

Azərbaycan Arxeologiyası 2000

Azerbaijan Archeology Vol.: 2 Num.: 3-4

Kabala and Gyandja had the following types: transparent, fritted, low-melting consisting of secondary clays from old-terrace deposits. There are 7 kinds of everyday glazed earthenware:

- Leaden;

- low-leaden;

- leaden-tin;

- low-tin;

- low-leaden-tin;

- leaden-low-tin;

- silicate.

Why were there in above - mentioned developed cities used 7 kinds of everyday glazed earthenware with toxic leaden-tin glazes?Firstly, oxides of lead impart to glazes some valuable properties, namely: a) fusibility; b) glance; c) high mechanical property except for hardness; d) elasticity.

Secondly, we may now assert that these earthenware were not contiguous to food-stuffs.

Thirdly, leaden everyday earthenware at high temperatures lost in some cases their toxicity.

To manufacture glazed earthenware in the Middle Ages, opaque glaze to give no opportunity to study structure of earthenware by their crocks. " To produce opaque glaze they often admix a lead to calcite obtained by means of combined burning of lead in the mixture with tin (ratio, from 2:1 to 6:1)".Ancient articles of these alloys are found in the monuments of so called "tin stage" in the history of metals.1

2

3

4 Dioxide of tin (Sn02) favourably affects elastic and thermal properties of glaze, increases its chemical resistibility.Main component of composition of faience glaze found in Shabran is copper (ratio; from 2,45 to 4,66; atomic and molecular weights are 79,6 ). Rarely met are compounds of spinel chromium type (Cr-from 0,017 to 0,65%. Atomic and molecular weights are 52,0 ) and that of cobalt (Co-from 0,90 to 0,035%; atomic and molecular weights are 59,9).

In some faience crocks and glazes light (colour). Hence it follows that a temperature of burning is below 950°C. " At a temperature of 950°C glaze has a copper oxide and frits of gray colour is formed".5

6 It must be noted that copper content in the composition of blue glazes of the glazed earthenware of Gyandja is less (from 0,020 to 0,20% ) than that found in Shabran. Usage of chromium green in ceramic manufactures relates to complex dyes. By its character and nature it is easier adapted in silicates. Besides, its application is limited because of its quick solubility in water.

In the composition of Gyandja dark blue faience glazes cobalt concentration is more ( from 0,040 to 0,085% ), in Shabran samples is less (0,035% ). Copper (0,039-1% ) and cobalt ( 0,017-0,085% ) compounds are dyes of the glazed earthenware too. Also used are chromium (0,014-1% ) and manganese (0,14-0.35% ) compounds (Atomic and molecular weights are 54,9 ).

Azərbaycan Arxeologiyası

47

Azerbaijan Archeology

2000

Vol.: 2 Num.: 3-4

Chemical composition Of faience glazes (transparent, fusible and frit) in plain Shabran and mountainous Kabala is as follows.

Shabran

Si20-61.53-83.78% A1203-0.86-3.50 Fe203-0.67- 1.20 CaO-3.99-7.60 MgO-2.11 -4.05 Na20-3.05-4.14 K20-2.13-3.37

Kabala Si20-68.48-81.84% A1203- 4.99 -0.40 -2.77

Fe203-0.40-2.77 CaO - 1.99-4.74 MgO - 1.20-6.47 Na20- 1.20-6.47 K20-2.91 -4.46

Analogical variety in faience ceramic earthenwares composition is practically observed nowhere. Earthenware discovered, most of all, approximate to Nakhichevan finds.By silica ( Sİ2O ) content, earthenware of both cities are analogical. However, as is seen in Table, glazed earthenware of Shabran and Kabala differ greatly by content of alumina ( AI2O3 ). Here AI2O3 ensures clay refractoriness while increase

о

of K2O and Na20 content points out to their fusibility. It has been established that acid low - temperature clays were burned till 1100°C.7

9 Increased content of ferrous oxide points out that in the glazed earthenware bentonides had been used most frequently. Their binding power is 2-2,5 times higher than that of other colloid clays. Shabran everyday faience is brittle with reduced chemical resistibility in comparison of glaze. There is an oversandness of raw material in Shabran and Kabala faience glaze. An increase of Sİ2O to 80% and more points to oversandness.10 Composition of raw material, its physical and chemical, mechanical and aesthetical material indices have been revealed.

At present some archaeologists and historians, taking no into consideration rapid economic development of the Middle Ages, are inclined to think that if there are not written and material sources on any branch of production, such as glazed earthenware, then local manufacture of the glazed earthenware is impossible. The discovery 0 non-deformed glazed earthenware at archaeological excavations is erroneously explained by the assertion that these wares are "imported".

Functionality of each new everyday thing of the Middle Ages is to be considered not separately but as an integral whole.

A study of material evidence needs for more complex and right method - a maximal usage of potentialities of integrated sciences.

■

Bibliography

- Tcherpushkin I.T. Production of coloured ceramic earthenware. State Publishing House of the North Ossetic Autonomous Soviet Socialist Republic. Dzaudjikau, 1948, p.71

- Ragimova M.N. From the history of lead usage in ancient and medieval Azerbaijan, Baku, "Elm", 1978;

- Blumen L.M. Glazes. Moscow, State Publishing House of Literature on Building Materials, 1954, p.86

- Ragimova	,p.63.

- Blumen	,p.86.

- Ibid...., p.40.

- Archaeology and natural sciences. M., 1965. - In: N. S. Gradjankina. Methods of chemical-technological investigation of ancient ceramics, p. 159. table 2.

ELMLƏRJN İNTEQRASİYASIVƏ ŞİMALİ AZƏRBAYCANDA FAYANS ISTEHSALININ ÖYRƏNMƏ METODLARI

Н.Теутигоц, H.Ramazanlı

Xülasə

Araşdırmada cəmiyyətin ictimai-siyasi inknşafın aparıcı roluna malik olan elmi-texniki tərəqqidin imkanları təhlil edilir. Şimali Azərbaycan arxeologiyasına aid tədqiqadlarda elmlərin qovuşması amili böyük üstünlüyə malikdir. Burada qısa, konkret formada təbii, texniki, psixoloji və humanitar sahələr bir-birinə elmi əsaslarla qovuşur. Tədqiqatlarda Şimali Azərbaycanda fayans istehsalına aid təsadüfı çox kiçik, ikinci dərəcəli faktlara rast gəlmək mümkündür. Son vaxtlar elmlərin aparıcı metodlarının köməyi sayəsində indiyə qədər həlli mümkün olmayan məsələlər müvəfəqiyyətlə araşdırılır və təhlil edilir.